## Slide 1
Quantum World at Atomic Scale:
Spin-Polarized Scanning Tunneling Microscopy
1. Institute of Applied Physics, University of Hamburg, Jungiusstrasse 11, D-20355 Hamburg, Germany
2. Department of Physics, National Tsing Hua University, No. 101, Section 2, Kuang-Fu Road, Hsinchu 30013, Taiwan
Pin-Jui Hsu1,2 (徐斌睿)
H/ Fe-DL/ Ir(111)
Fe-DL/ Rh(001)
Fe-TL/ Ir(111)

## Slide 2
Spin-Polarized STM
Working Principle

## Slide 3
Spin-Polarized STM
Working Principle
Mn/ W(110)
Topo.
Cr(001)
dI/dU

## Slide 4
Spin-Polarized STM
Magnetic Domain Wall
Bloch Wall
Neél Wall

## Slide 5
Spin-Polarized STM
Magnetic Domain Wall, AFM Cr(001)
Cr(001)
R. Wiesendanger, Rev. Mod. Phys., 81, 1495 (2009)

## Slide 6
Spin-Polarized STM
Magnetic Domain Wall, FM Fe-DL/W(110)
R. Wiesendanger, Rev. Mod. Phys., 81, 1495 (2009)

## Slide 7
Spin-Polarized STM
Magnetic Domain Wall, FM Fe-DL/W(110)
O. Pietzsch et al., Science, 292, 2053 (2001)

## Slide 8
Spin-polarized States
Spin-polarized Surface State, FM Co-DL/Cu(111)
O. Pietzsch et al., Phys. Rev. Lett., 92, 057202 (2004)
L. Diekhöner et al., Phys. Rev. Lett., 90, 236801 (2003)
H. Oka et al., Science, 327, 843 (2010)
Topography Z(x,y)
Conduc. dI/dU(x,y)

## Slide 9
Spin-Polarized STM
Atomic Spin Resolution, AFM Fe-ML/W(001)
A. Kubetzka et al., Phys. Rev. Lett., 90, 236801 (2003)

## Slide 10
Spin-Polarized STM
Atomic Spin Resolution, AFM Mn-ML/W(110)
M. Bode et al., Nature, 447, 190 (2007)

## Slide 11
Magnetic Skyrmion
Dzyaloshinsky-Moriya Interaction
DMI has the dominant contributions to formation of magnetic skyrmion spin texture.
A, Fert, V. Cros, and J. Sampaio, Nature Nano., 8, 152 (2013)
The current density required to move skyrmions has 5~6 order of magnitudes smaller than DW movement.
Non-trivial topology and lower depinning currents lead to low energy consumption.

## Slide 12
Spin-Polarized STM
Magnetic Phase transition, Magnetic Skyrmions
N. Romming et al., Science, 341, 636 (2013)
P. J. Hsu et al., Nat. Nano., 12, 123 (2017)

## Slide 13
J, Barker, and O. A. Tretiakov, Phys. Rev. Lett., 116, 147203 (2016)
A. K. Nayak, V. Kumar, P. Werner, E. Pippel, R. Sahoo, F. Damay, U. K. Roßler, C. Felser, and S. P. Parkin, Nature, 548, 561 (2017)
B. Dupé, C. N. Kruse, T. Dornheim, and S. Heinze, New. J. Phys., 18, 055015 (2016)
Magnetic Skyrmion
AFM skyrmion; Antiskyrmion; |Q| > 1

## Slide 14
Single-Atom Magnetometry
SP-STM/STS with B field, Co atoms/Pt(111)
F. Meier et al., Science, 320, 82 (2008)

## Slide 15
Single-Atom Magnetometry
Moving Single Atoms
M. F. Crommie et al., Science, 262, 218 (1993)
75 Fe/ Cu(111)
34 Xe / Ni(110)
CO/ Cu(111)

## Slide 16
Single-Atom Magnetometry
Moving Single Atoms, Lateral Movement
S. W. Hla, J. Vac. Sci. & Tech. B, 23, 1351 (2005)

## Slide 17
Single-Atom Magnetometry
Moving Single Atoms, Vertical Manipulation
K. K. Gomes et al., Nature, 483, 306 (2012)
271 CO/ Cu(111)

## Slide 18
Moving Single Atoms
Spin Logic Operations
A. Khajetoorians et al., Science, 332, 1062 (2011)

## Slide 19
SP-STM with Time Resolution
Single-Atom Dynamics
S. Baumann et al., Science, 417, 350 (2015)
T. Choi et al., Nat. Nanotech., 12, 420 (2017)
F. D. Natterer et al., Nature, 543, 226 (2017)

## Slide 20
Summary & Future Highlights
There are more to explore !!
Thanks for your attention !